­___
Alan McGaughey
Associate Professor
Department of Mechanical Engineering
Carnegie Mellon University
Pittsburgh, PA 15213-3890
Tel: (412) 268-9605
Fax: (412) 268-3348
Email: mcgaughey@cmu.edu
March 22, 2013
Dear Physical Review B Editor:
We are submitting the manuscript titled “Evaluation of the virtual crystal approximation for predicting alloy vibrational mode properties and thermal conductivity” by Jason M. Larkin and Alan J. H. McGaughey for consideration for publication in Physical Review B.
Due to their low thermal conductivities, alloys are currently an active area of research, notably in the thermoelectric energy conversion field. The ability to predict alloy thermal conductivity is critical in narrowing down a large materials design space. Recent papers [e.g., PRL 106, 045901 (2011), PRL 109, 095901 (2012), PRB 85, 184303 (2012)] have used anharmonic lattice dynamics and the virtual crystal approximation (an approach we call VC-ALD) to make such predictions.
In VC-ALD, the disorder in the alloy is treated as a perturbation. The limits of this approach have yet to be determined. In our work, we use computationally-inexpensive empirical potentials to assess the virtual crystal approximation by self-consistently treating the disorder explicitly and as a perturbation. We are not aware of any such previous study. Our results indicate that while VC-ALD is generally an accurate method, care must be taken when modeling alloys with low thermal conductivities, where significant underprediction of thermal conductivity is likely.
Reference numbers correspond to those used in our submitted manuscript.
1) The breakdown of the VC-ALD method, specifically the phonon-defect scattering theory of Tamura.  We believe that this breakdown has gone unnoticed by other studies using VC-ALD because they have focused on low-frequency dominated materials or have not carefully compared with experiment.\cite{lots of PRB articles}  Our study is self-consistent and includes 2 example materials which demonstrate the applicability and breakdown of the VC-ALD method.
2) The application of the AF theory of diffusons to a disordered lattice, which has not been done before.\cite{lots of PRB articles}  This application allowed us to identify the high-scatter limit for vibrational diffusivity in a disordered lattice, which was essential for identifying the breakdown in the VC-ALD method.  This high-scatter limit of diffusivity is usually assumed, without theoretical justification, in models for disordered and amorphous materials.\cite{PRB articles}
3)  The measurement of the structure factor for modes in a disordered lattice, which has only been done previously for amorphous materials.\cite{PRB articles} This allowed us to identify the underprediction o the VC-predicted group velocity as the representative velocity scale for mode diffusivities in the disordered lattice.

We suggest the following reviewers:
Davide Donadio
Group Leader
Max Planck Institute for Polymer Research
donadio@mpip-mainz.mpg.de
Junichiro Shiomi
Associate Professor
Mechanical Engineering, University of Tokyo
shiomi@photon.t.u-tokyo.ac.jp

Xiulin Ruan
Assistant Professor
Mechanical Engineering, Purdue University
ruan@purdue.edu
We look forward to your response.
Sincerely,

Alan McGaughey